## Slide 1
Timber Defects
Lecturer: James Rix

## Slide 2
Aims & Objectives.
Aims:
Objectives:
Describe different types of defects found in timber products
Define natural Defects in Wood
Outline conversion defects in Wood
Identify seasoning defects in wood
Examine Fungal defects in wood
Determine insect defects in wood

## Slide 3
Wood Defects.
A defect is an irregularity or abnormality found in or on wood. These defects are caused for several reasons, see the diagram below.
Wood Defects
Natural
Conversion
Seasoning
Fungi
Insects
All defects affect the wood and in different ways, but they are all responsible for the following:​
​
The strength of the wood is reduced​
The durability is lowered​
The utility is lowered​
They give poor appearance​
They cause decay in the wood​

## Slide 4
Natural Defects

## Slide 5
Natural Defects.
Burr’s
Callus
Coarse Grain
Chemical Stain
Deadwood
Druxiness
Foxiness
Knots
Rind Galls
Shakes
Twisted Fibres
Upsets
Resin Pockets
Wind Cracks
Natural defects in wood are defects that occur naturally, these are defects that have happened during the tree’s growth by some type of natural outside force.

## Slide 6
Burr’s
While in its infancy a tree can receive shock or injury, a burr is a result of the tree undergoing some form of stress. The grain grows in a ​deformed manner filled with ​small knots.
Burr Walnut
Burr Ash
Burr Oak
Burr’s are highly figured wood ​
and sort after. They are sliced into veneers and used for furniture and inlays in doors.​
Burr’s are hard to work with due to the twisty tight grain. The wood is incredibly dense and is prone to chipping and shattering.

## Slide 7
Callus
A callus forms when the tree is damaged and has a wound. The wound is sealed by the callus in order for it to begin to heal. It is a soft tissue that surrounds the wound.

## Slide 8
Chemical Stain.
Sometimes wood is discoloured by an external agency. The external agent like the gasses present in the atmosphere can discolour the wood. This is known as chemical stain.
Chemical Stain

## Slide 9
Coarse Grain.
Coarse grain happens when a tree grows rapidly, by doing this the annual rings are widened which also weakens the wood and gives it a coarse texture.
Widened annual rings

## Slide 10
Deadwood.
Dead wood is wood that is light red in colour and comes from a tree that though still standing, is dead or has dead parts. Dead wood can remain in living trees for many years and can be fatal to the tree. Dead branches should be removed from the tree to reduce the risk of injury from falling off the living tree and hitting someone who may be passing by.

## Slide 11
Druxiness.
Druxiness appears ​as white spots on the ​tree which can be ​concealed by healthy ​wood. The white spots allow access for fungi to grow.
Druxiness

## Slide 12
Foxiness.
Foxiness is a discolouration in the timber around the pith. It is identifiable by a red or yellow tinge or spots or red or yellow stains. The discolouration is due to poor ventilation during the storage of the timber.
Foxiness
Logs all marked with foxiness.

## Slide 13
Knots 1 – Live & Dead Knots.
Fixed into the wood and cannot be separated, free from cracks or decay and this kind of knot can be used in wood used for engineering purposes.
Live knots.
Dead knots.
Annual rings are not intergrown with surrounding wood, it is not safe to use wood containing dead knots for engineering purposes.
In accordance with ISO2299.

## Slide 14
Knots 2 – Sound, Unsound & Rotten Knots.
Sound knots.
Knots showing no signs of decay and are classified as light or dark knots.
Unsound knots.
Knots in which not more than a third of the cross section is rotten.
Rotten knots.
Knots in which more than a third is rotten.
In accordance with ISO2299.

## Slide 15
Knots 3 – Round, Oval & Splayed Knots.
In accordance with ISO2299.
Round knots.
Knots cut so that the ratio between the maximum and the minimum diameters is not more than 2
Oval knots.
Knots cut so that the ratio between the maximum and the minimum diameters is more than 2 but not more than 4
Splay knots.
Knots cut so that the ratio between the maximum and the minimum diameters exceeds 4

## Slide 16
Knots 4 – Face, Edge, Arris & Traversing Splay Knots.
In accordance with ISO2299.
Face knots.
Knots that are exposed on the face of the wood.
Edge knots.
Knots that are exposed on the edge of the wood.
Arris knots.
Knots that are exposed on the Arris of the wood.
Traversing Splay knots.
Knots that are exposed on two arisses of the same piece of wood simultaneously.

## Slide 17
Knots 5 – Scattered, Group, Branched & Intergrown Knots.
In accordance with ISO2299.
Scattered knots.
Knots located separately and so that the distance between them is greater than its width.
Group knots.
Round, oval and Arris knots forming a group of two or more knots in an area whose length is equal to its length.
Branched knots.
Two splay knots on the same axis equal to the width of the wood.
Intergrown knots.
Knots with their annual rings intergrown into surrounding wood.

## Slide 18
Knot Size Classification
Up to 6.5mm
Pin Knot
6.5mm to 19mm
20mm to 39mm
40mm +
Small Knot
Medium Knot
Large Knot

## Slide 19
Resin Pocket.
During the tree's growth a tree may be damaged, cavities can form in between the rings of the tree that fill with a resin. This resin is produced by all trees. In coniferous trees the resin is a yellow like sticky substance and is used for oils and incense and contain many essential oils. Deciduous trees contain a transparent resin which is used for varnishes and adhesives. Tree resin is used worldwide for more than 5000 purposes.

## Slide 20
Rind Galls.
Rind Gall
Rind = Bark
Galls = Abnormal growth
A rind gall produces a peculiar swelling in the body of the tree. They will form where branches have either been improperly removed or have fell away. The timber produced by the tree in this area is very weak and not very durable.

## Slide 21
Shakes - Ring.
A ring shake is a timber defect where the wood splits along one of its annual growth rings, creating a circular or curved crack inside the trunk. This separation usually forms while the tree is still growing, often caused by internal stresses such as rapid temperature changes, strong winds, or sudden growth spurts. It can also result from bacterial infection or frost damage weakening the bond between growth layers. Ring shakes reduce the strength and durability of timber, making affected wood unsuitable for structural use but still useful for decorative or non-load-bearing applications.

## Slide 22
Shakes - Heart.
A heart shake is a split that radiates outward from the centre (heartwood) of the tree, often forming star-like cracks through the core. These shakes develop as the tree ages, and the heartwood begins to shrink or lose moisture faster than the surrounding layers. Internal stresses, frost, or rapid drying can cause the wood fibres to separate along the grain. Heart shakes weaken the timber’s structural integrity, making it unsuitable for load-bearing uses but still acceptable for smaller or decorative components where strength is less critical.

## Slide 23
Shakes - Star.
A star shake is a type of timber defect where multiple cracks radiate outward from the centre of the tree trunk, forming a star-like pattern. These splits usually occur due to internal stresses caused by rapid drying, frost, or strong winds while the tree is growing or seasoning. The cracks separate the wood fibres along the grain, weakening the timber’s structural integrity. Star shakes are common in older trees and can extend deep into the heartwood, making the affected timber unsuitable for structural use but still usable for smaller or decorative applications.

## Slide 24
Twisted Fibres.
A twisted fibre defect occurs when the wood grain spirals around the trunk instead of running straight along its length. This happens as the tree grows unevenly, often due to persistent wind pressure, uneven sunlight exposure, or the tree leaning on a slope. The fibres follow this spiral growth pattern, creating timber that is difficult to saw, plane, or split cleanly. Twisted grain reduces the wood’s strength and stability, making it prone to warping and distortion during drying or use in construction.

## Slide 25
Water Stains.
A water stain defect appears as discoloured patches or streaks on the wood surface, often grey, blue, or dark brown. These stains form when water penetrates the timber, reacting with tannins and minerals inside the wood. They can occur while the tree is still standing — from rain or groundwater — or after felling, during storage or seasoning. Although water stains rarely affect the wood’s strength, they spoil its appearance and can make finishing or polishing difficult, especially in decorative or furniture-grade timber.

## Slide 26
Wind Cracks.
Wind cracks are splits that form in a tree’s trunk due to strong, uneven wind pressure acting on the stem over time. When gusts repeatedly bend or twist the tree, internal stresses build up within the wood fibres. If the stress becomes too great, the fibres separate, creating long, radial cracks that run from the centre of the trunk outward. These cracks weaken the structural integrity of the timber and can extend deep into the heartwood, making affected logs unsuitable for load‑bearing uses.

## Slide 27
Conversion Defects

## Slide 28
Chip Mark.
Chip marks occur when small sections of wood are torn or ripped from the surface during machining, typically while planing or sawing. This defect happens when the grain direction opposes the cutting motion, causing fibres to lift and break away instead of slicing cleanly. The result is a rough, uneven patch that spoils the smooth finish and may weaken the timber’s surface integrity. Good tool maintenance, correct feed speed, and cutting with the grain help reduce chip marks and ensure a cleaner, more professional finish.

## Slide 29
Diagonal Grain.
Diagonal grain is a conversion defect where the grain of the timber runs at an angle instead of parallel to the length of the board. This usually happens when the log is not sawn straight or when the cut passes through the tree’s growth rings at an angle. As a result, the board shows slanted grain lines, which can weaken the timber and make it more prone to warping or splitting under load. Diagonal grain also reduces the visual quality of the wood and can affect how it machines, making it less suitable for precision construction work.

## Slide 30
Torn Grain.
Torn grain is a conversion defect that occurs when the cutting blade tears out fibres instead of slicing them cleanly, leaving rough, uneven patches on the timber’s surface. It often happens when working against the grain, using dull or poorly set blades, or machining timber with interlocked or difficult grain patterns. Torn grain not only affects the appearance of the wood but can also weaken the surface, making it harder to achieve a smooth, accurate finish. Extra sanding, planing, or re‑machining is usually needed to correct the defect and restore a workable surface.

## Slide 31
Wane.
Waney Edge Explained A waney edge refers to the natural, uneven edge of a plank where the bark and original contour of the tree are left intact. Rather than being sawn square, this edge preserves the organic shape and texture of the timber, showcasing the transition from rough bark to smooth heartwood. It’s often used in furniture making, shelving, and decorative joinery to highlight the authenticity and character of the wood. Each waney-edged board is unique, revealing the tree’s growth patterns and adding a rustic, handcrafted aesthetic that connects the finished piece back to its natural origin.

## Slide 32
Seasoning Defects

## Slide 33
Bowing.
Bowing is a conversion defect that occurs when a piece of timber curves along its length, creating a gentle, outward bend from end to end. It usually develops because of uneven drying, where one face of the timber loses moisture faster than the other, causing internal stresses that pull the board into a curve. Poor storage, high humidity changes, or using timber with natural growth stresses can all increase the risk. Bowed timber is harder to fix in place accurately and often needs to be re‑machined, cut down, or rejected to ensure accurate construction work.

## Slide 34
Cupping.
Cupping is a conversion defect where a timber board curves across its width, creating a shallow “U” shape as the edges lift higher than the centre. It happens when one face of the timber dries faster than the other, causing uneven shrinkage that pulls the board into a curved profile. Poor stacking, exposure to moisture changes, or cutting too close to the tree’s growth rings can all increase the risk. Cupped boards are difficult to fix flat and often need to be re‑machined, planed down, or rejected to ensure accurate and stable construction work.

## Slide 35
Crook.
Crook is a conversion defect where a timber board bends along its edge, creating a sideways curve when viewed from above. Unlike bowing, which runs along the flat face, crook affects the narrow edge, causing the board to veer left or right. It usually develops because of uneven drying, natural growth stresses, or poor storage conditions that allow one side of the board to shrink more than the other. Crooked timber can be difficult to align accurately in frames or long runs and often needs to be re‑sawn, planed, or trimmed to restore a straight edge suitable for construction work.

## Slide 36
Twisting.
Twisting is a conversion defect where a timber board rotates along its length, causing each end to turn in opposite directions so the piece no longer sits flat. This defect usually develops when the timber dries unevenly, especially if the growth rings are angled or the board contains internal stresses from the tree. Poor stacking, inconsistent airflow, or storing boards without proper support can make twisting worse. Twisted timber is difficult to use accurately because it won’t lie flat against surfaces, often requiring re‑machining, cutting down, or rejection to ensure reliable construction work.

## Slide 37
Case Hardening.
Case hardening is a conversion defect that occurs when the outer layers of a timber board dry much faster than the inner core, creating internal tension. As the surface shrinks and stiffens prematurely, the core remains swollen with moisture, leading to stress that can cause the board to warp, cup, or even split when cut or machined. This imbalance often results from improper kiln‑drying, where temperature and airflow are not controlled evenly. Timber affected by case hardening can be difficult to work with, as releasing the internal stresses during cutting may cause sudden movement or distortion, reducing accuracy and structural reliability.

## Slide 38
Split.
Splitting is a conversion defect where timber separates along the grain, creating cracks that run in from the ends of the board. It usually happens when the wood dries too quickly or unevenly, causing the fibres to pull apart under internal stress. Poor handling, end‑grain exposure, or using timber with natural weaknesses can make splitting more likely. Once splits develop, they reduce the board’s strength and stability, often requiring the damaged section to be cut off or the piece to be rejected for accurate construction work.

## Slide 39
Shakes.
Shakes are a conversion defect where timber develops separations or cracks along the grain, often forming before or during the conversion process. They occur when internal stresses in the tree—caused by rapid growth, frost, drought, or age—cause the wood fibres to split apart. These cracks can appear as heart shakes, ring shakes, or star shakes, depending on their pattern and location within the log. Shakes weaken the structural integrity of the timber, reduce usable yield, and often make affected boards unsuitable for high‑quality or load‑bearing construction work.

## Slide 40
Checks.
Checks are a conversion defect where small, fine cracks form on the surface of timber, usually running along the grain. They occur when the outer layers of the wood dry and shrink more quickly than the inner core, creating tension that causes the surface to split. Checks are typically shallow and don’t run all the way through the board, but they can still weaken the timber’s appearance and reduce its suitability for high‑quality finishing. Poor drying control, rapid moisture loss, or exposure to harsh environmental changes all increase the likelihood of checking during the conversion process.

## Slide 41
Fungi Defects

## Slide 42
Dry Rot.
Dry rot is a fungal defect caused by the fungus Serpula lacrymans, which attacks timber with a moisture content typically above 20%. It breaks down the cellulose within the wood, leaving it dry, brittle, and crumbly, often with a distinctive cubed cracking pattern. As the fungus spreads, it can produce cotton‑like mycelium and red‑rust fruiting bodies, allowing it to travel across masonry in search of new timber to feed on. Dry rot is one of the most serious timber defects because it can rapidly weaken structural elements, requiring both the source of moisture to be eliminated and the affected timber to be removed or treated to prevent further decay.

## Slide 43
Wet Rot.
Wet rot is a fungal defect caused by fungi such as Coniophora puteana and Poria vaillantii, which thrive in timber with a consistently high moisture content, usually above 30%. Unlike dry rot, wet rot cannot spread through masonry and remains confined to damp timber, but it still causes significant damage by breaking down the wood’s cellulose and hemicellulose, leaving it soft, spongy, and darker in colour. Affected areas often show a cracked, fibrous texture and may crumble when pressed. Wet rot typically develops in places with persistent leaks, poor ventilation, or ground contact, and controlling the moisture source is essential before repairing or replacing the damaged timber.

## Slide 44
Blue Stain.
Blue stain is a fungal defect caused by staining fungi that penetrate the sapwood and leave it discoloured with blue, grey, or black streaks. Unlike decay fungi, blue‑stain fungi do not significantly weaken the structural strength of the timber, but they do affect its appearance, making it less suitable for visible or high‑quality finishes. The fungi thrive in freshly felled or poorly stored timber with high moisture content, often entering through the rays or vessels of the wood. Although the defect is mainly cosmetic, it can reduce the commercial value of the timber and indicates that storage or drying conditions need improving to prevent further fungal activity.

## Slide 45
Brown Rot.
Brown rot is a fungal defect that breaks down the cellulose in timber, leaving the wood dry, crumbly, and weakened. As the fungus consumes the structural fibres, the timber shrinks and fractures into distinctive brown, cube‑shaped pieces, a pattern often called cuboidal cracking. Brown rot thrives in persistently damp conditions, especially where ventilation is poor or moisture levels remain high. Although it does not spread through masonry like dry rot, it can still cause serious structural damage, and affected timber usually needs to be removed and the moisture source eliminated to prevent further decay.

## Slide 46
Heart Rot.
Heart rot is a fungal defect that attacks the heartwood at the centre of a tree, gradually breaking it down from the inside out. It is caused by fungi that enter through wounds in the bark—often from storm damage, pruning cuts, or insect activity—and slowly decay the inner core while the outer layers may still appear sound. As the rot progresses, the timber becomes soft, brittle, and structurally weakened, reducing the usable yield once the log is converted. Because heart rot develops while the tree is still standing, it can be difficult to detect until felling, and severely affected timber is usually unsuitable for structural or high‑quality construction work.

## Slide 47
White Rot
White rot is a fungal defect that breaks down both the cellulose and lignin in timber, leaving the wood soft, fibrous, and noticeably lighter in colour. As the fungus digests these structural components, the timber often develops a whitish, stringy, or spongy texture, sometimes with dark zone lines running through it. White rot thrives in damp, poorly ventilated environments where moisture levels remain high for long periods. Although it progresses more slowly than brown rot, it can still cause serious structural weakening, and affected timber usually needs to be removed once the moisture problem has been resolved.

## Slide 48
Insect Defects

## Slide 49
Beetles.
Ambrosia Beetle.
House Longhorn Beetle.
Furniture Beetle.
Wood Wasp.
Ambrosia beetles are tiny wood‑boring insects that cultivate and feed on a specialised fungus they carry into the trees they infest. Although small, they can cause significant damage to weakened or stressed trees by tunnelling through the wood and introducing their fungal gardens.
Furniture beetle, often called woodworm, is a small brown beetle whose larvae bore tiny round holes through softwood timbers and furniture. The larvae can live inside the wood for several years, gradually weakening structural or decorative pieces as they feed.
The house longhorn beetle (Hylotrupes bajulus)** is a wood‑boring insect commonly found in softwood timbers used for roof structures and joinery. Its larvae tunnel deep into the wood, leaving oval exit holes and powdery frass as they feed. Over time, this activity weakens structural components, particularly in older buildings. The adult beetle is dark brown to black with long antennae and mottled wing cases, often emerging during warm months when infestations become visible.
A wood wasp, or horntail, is a large, harmless insect whose larvae bore into softwood like pine and spruce. The female lays eggs deep in the timber using a long ovipositor, often introducing a fungus that helps the larvae feed. As they tunnel, they leave smooth, round holes that can weaken the wood, though they pose no risk to people.

## Slide 50
House Longhorn Beetle.
House Longhorn Beetle.
The house longhorn beetle (Hylotrupes bajulus)** is a wood‑boring insect commonly found in softwood timbers used for roof structures and joinery. Its larvae tunnel deep into the wood, leaving oval exit holes and powdery frass as they feed. Over time, this activity weakens structural components, particularly in older buildings. The adult beetle is dark brown to black with long antennae and mottled wing cases, often emerging during warm months when infestations become visible.

## Slide 51
Ambrosia Beetles.
Ambrosia Beetle.
Ambrosia beetles are tiny wood‑boring insects that cultivate and feed on a specialised fungus they carry into the trees they infest. Although small, they can cause significant damage to weakened or stressed trees by tunnelling through the wood and introducing their fungal gardens.

## Slide 52
Furniture Beetles.
Furniture Beetle.
Furniture beetle, often called woodworm, is a small brown beetle whose larvae bore tiny round holes through softwood timbers and furniture. The larvae can live inside the wood for several years, gradually weakening structural or decorative pieces as they feed.

## Slide 53
Wood Wasp.
Wood Wasp.
A wood wasp, or horntail, is a large, harmless insect whose larvae bore into softwood like pine and spruce. The female lays eggs deep in the timber using a long ovipositor, often introducing a fungus that helps the larvae feed. As they tunnel, they leave smooth, round holes that can weaken the wood, though they pose no risk to people.

## Slide 54
Marine Borers.
Marine borers are wood‑eating marine organisms—such as shipworms and gribbles—that tunnel into submerged timber like piers, jetties, and wooden hulls. Their constant feeding can rapidly weaken structures below the waterline, making them a major concern in coastal construction and marine engineering.

## Slide 55
Termites.
Termites are social insects that live in large colonies and feed primarily on cellulose found in wood and plant material. If left untreated, their hidden tunnelling and constant feeding can cause serious structural damage to buildings and timber elements.

## Slide 56
Recap.
Defined natural Defects in Wood
Outlined conversion defects in Wood
Identified seasoning defects in wood
Examined Fungal defects in wood
Determined insect defects in wood

## Slide 57
Any Questions?
If you have any questions why not try and look up the answer online using a search engine and typing in your question, if you cant find your answer then ask your tutor or email them your questions at:
Lecturer@college.ac.uk

## Slide 58
Thank You.
We would like to take this opportunity to thank you for using this material. If you have any questions or suggestion on this or any other learning material produced by Educon please email:
Educon.rix@gmail.com
Lecturer: James Rix